## Slide 1: The superexchange interaction in overdoped manganites
L.E. Gonchar
Ural State University of Railway Transport
Ural Federal University named after First President of Russia B.N. Yeltsin,
Yekaterinburg, Russia

## Slide 2: Model of the JT magnetic crystal
Crystalline structure,
charge ordering (experimental data from papers)
Orbital ordering
Linear vibronic interaction
Orbitally-dependent superexchange interaction & SIA
Tuning of model*
Magnetic structure
*If necessary, the non-linear and non-local parts could be added to the model. These part are not used in current investigation,

## Slide 3: Orbital subsystem model
Mn3+ d4, in the crystal field of octahedron 5E, eigenfunctions: |~2z2-x2-y2, |~x2-y2
HJT=Ve(QX+QX)
d4
5E
t2g
eg
angle parameter characterizing the orbital state of Mn3+ - the main in the work
Ve= –1,29 эВ/Å*
* | A.E. Nikiforov, S.E. Popov Appl. Phys. A 74, S1743 (2002)
Q
Q

## Slide 4: Symmetrized eg-distortions and orbital structures
La1/3Ca2/3MnO3, Pnma3
Mn3+5E
Mn4+ 4A2
Q1=Q3»2p-Q2=2p-Q4=Q
structure from Radaelli P.G. et al. PRB 59,14440 (1999)
La1/4Ca3/4MnO3, P21/m
Bi1/5Ca4/5MnO3, Pnma5
structure from S. Grenier et al. PRB 75 085101 (2007)
structure from M. Pissas et al. PRB 72, 064426 (2005)

## Slide 5: Magnetic subsystem model
+ transformation of the reference frame from local axes of octahedron to general system

## Slide 6: Orbitally-dependent exchange interaction
Mn3+ – Mn3+ (x, y, z)
Mn3+ – Mn4+ (x, y, z)
Mn4+ – Mn4+
Mn3+
O2-
Mn3+

## Slide 7: Parameters of interactions
Compound | Parameters, meV
La1/3Ca2/3MnO3 (=5/3) | J3ac=1.0, J2ac,1=2.2, J2ac,2= 9.1, J3b=1.3, J1b=2.4 D=0.15, E=0.15
La1/4Ca3/4MnO3 (=1.58) | J3ac=1.0, J2ac,1=2.6, J2ac,2= 9.7, J3b=1.3, J1b=1.4 D=0.08, E=0.17
Bi1/5Ca4/5MnO3 (=1.66) | J3ac=1.2, J2ac,1=3.4, J2ac,2= 9.0, J3b=1.3, J1b=1.3 D=0.14, E=0.15

## Slide 8: Orbital dependence of superxchange interaction and exchange energy
z
Wide arrows show the orbital mixture angles of the experimental structures [Radaelli P.G. et al. PRB 59,14440 (1999), M. Pissas et al. PRB 72, 064426 (2005), S. Grenier et al. PRB 75 085101 (2007)]
Magnetic structures of types 1 and 2 are complicated. They are drawn in slide 9.

## Slide 9: Magnetic structures (next pane –opposite directions)
Compound | 1- kc=0 ¦¦ | 2 - kc={0,0,1/2} ¦¦ 
La1/3Ca2/3MnO3 FM trimers |  | 
La1/4Ca3/4MnO3 FM trimers FM stripes (AFM stripes) |  | and some others
Bi1/5Ca4/5MnO3 FM trimers AFM stripes |  | and some others

## Slide 10: Magnetic structure: comments
The main differences between 1 and 2 magnetic structures are:
  the propagation wave vector of magnetic structure in c direction
    kc=0 for 1 structure;
    kc={0, 0, ½} for 2 structure;
  the AFM frustrated bonds (Mn3+ =2, Mn4+ )
    Mn3+ Mn4+ for 1 structure ();
    Mn4+ Mn4+ for 2 structure ();
The regions of  are (approximately, due to orbital part only):
  0/3, 5/32 for 1 structure;
  /30.69, 1.315/3 for 2 structure;
  0.691.31 for G structure.
There are lots of non-collinear structures in 2 orbital-mixing-angles region, a choice could be made using single-ion anisotropy with tilting account.

## Slide 11: Magnetic structure: La1/3Ca2/3MnO3
Comparing with experiments (Radaelli, PRB59 14440, Fernández-Díaz, PRB59 1277(1999)) :
Wave vector of MS
Magnetic trimers, angle between trimers 800 (56о –Radaelli, 80о- Fernández-Díaz)

## Slide 12: Conclusions
Model describes various magnetic structures of JT insulating manganites
Magnetic subsystem is dependent upon orbital one
Orbital dependence afford to describe both general ordering and non-collinear components of magnetic structure
The main feature of magnetic structure: FM trimers with Mn4+ - Mn4+ planar bond frustration
NO C-structure

## Slide 13: Thank you for attention!
Liudmila E. Gonchar, Yekaterinburg, Russia
l.e.gonchar@yandex.ru
https://www.researchgate.net/profile/L-Gonchar-2

## Slide 14: Model is published in…
J.Magn.Magn.Mater. 465, 661 (2018)
Physics of the Solid State 61, 728 (2019)
J.Magn.Magn.Mater. 513, 167248 (2020)
Low Temp.Phys. 48, 37 (2022)
Phys. Met. Met. 123, 268 (2022)
Appl Magn. Reson. 54, 503–511 (2023)